Test 6 probe 1

|  |  |
| --- | --- |
| Program used | A white sheet with black text |
| Materiel used | UPI Good mems nonfunctional  UPI tube  UPI Circular alignment fixture  UPI dead weight |
| Result for vacuum | leaked |
| Result for over pressure | n/a |
| Reason for failure | Possibly contamination. I found a brown oily residue inside the tube |
| date | 11/2/2023 |
| operator | Jaikob Williams |
| Investigate by | Jaikob and Mich |
| notes | After attaching the mems to the pcb I did the normal cleaning cycle and after I cured the epoxy I cleaned the sub assembly again in acetone ,DI and IPA each for 10 minutes, and dried in the oven. I also cleaned the tubes a 2nd time. |